MOLEGRIDTM Washable

A basic resin that is easy to mold and can be cleaned with water.

Description

MOLEGRID™ Washable resin is designed with a washable formula, allowing models to be washed after molding, thus eliminating the need for alcohol or isopropyl alcohol cleaning. The resin has low odor, fast molding, and a high success rate in printing. It is compatible with various 3D printing equipment operating in the 405nm wavelength range.

Resion Color: black, white, gray, beige, Skin, transparent red, transparent orange, transparent green.

MOLEGRID™ Washable is widely used in model manufacturing, cultural peripherals, design, mold validation, and other fields, especially suitable for studios and individual gamers.

Characteristics

- Washable

- High precision, easy to mold

- Balanced strength and toughness

Recommended applications:

- Model manufacturing

- Design validation

- Cultural peripherals

| Liquid properties |  |  |  |
| --- | --- | --- | --- |
| Appearance | Transparent/Opaque | Density | 1.05-1.25g/cm3 @25℃ |
| Resin Viscosity | 100-350cps @25℃ |  |  |
| Mechanical properties |  | Post-cured 1 |  |
| ASTM Method | Properties Item | Metric Units2 | Imperial Units2 |
| D638 | Tensile Strength | 42.83MPa | 6.2ksi |
| D638 | Tensile Modulus | 2327.0MPa | 337.5ksi |
| D638 | Elongation at break | 11.47% |  |
| D790 | Flexural Strength | 71.48MPa | 10.37ksi |
| D790 | Flexural Modulus | 1959MPa | 284ksi |
| D256 | Impact value | 77.18J/m | 1.45ft-Ib/in |
| D2240 | Hardness(shore D) | 80-85D |  |
| Thermal properties |  |  |  |
| D648 | Heat deflection temperature@0.45MPa（66psi） | 60.8℃ | 141.4℉ |

1：The data was measured after post-curing for 30 minutes in a UV curing chamber with a light intensity energy density of 10 mW/cm².

2：The material properties may vary depending on the structure of the printed part, printing orientation, printing equipment, printing parameters, and post-curing process.