
MOLEGRIDTM Washable 

A basic resin that is easy to mold and can be cleaned with water.
Description
MOLEGRID™ Washable resin is designed with a washable formula, allowing models to be washed after molding, thus eliminating the need for alcohol or isopropyl alcohol cleaning. The resin has low odor, fast molding, and a high success rate in printing. It is compatible with various 3D printing equipment operating in the 405nm wavelength range.
Resion Color: black, white, gray, beige, Skin, transparent red, transparent orange, transparent green.

MOLEGRID™ Washable is widely used in model manufacturing, cultural peripherals, design, mold validation, and other fields, especially suitable for studios and individual gamers.
Characteristics
· Washable
· High precision, easy to mold
· Balanced strength and toughness
Recommended applications:
· Model manufacturing
· Design validation
· Cultural peripherals
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	Appearance
	Transparent/Opaque
	Density
	1.05-1.25g/cm3 @25℃

	Resin Viscosity
	100-350cps @25℃
	

	Mechanical properties
	Post-cured 1

	ASTM Method
	Properties Item
	Metric Units2
	Imperial Units2

	D638
	Tensile Strength
	42.83MPa
	6.2ksi

	D638
	Tensile Modulus
	2327.0MPa
	337.5ksi

	D638
	Elongation at break
	11.47%

	D790
	Flexural Strength
	71.48MPa
	10.37ksi

	D790
	Flexural Modulus
	1959MPa
	284ksi

	D256
	Impact value
	77.18J/m
	1.45ft-Ib/in

	D2240
	Hardness(shore D) 
	80-85D

	Thermal properties

	D648
	Heat deflection temperature@0.45MPa（66psi）
	60.8℃
	141.4℉




1：The data was measured after post-curing for 30 minutes in a UV curing chamber with a light intensity energy density of 10 mW/cm².
2：The material properties may vary depending on the structure of the printed part, printing orientation, printing equipment, printing parameters, and post-curing process.

